## Slide 1: Investigation of pulsed spin polarized electron beams at the S-DALINAC
PSTP 2013
PSTP 2013 - Martin Espig – 13.09.2013
M. ESPIG, J. ENDERS, Y. FRITZSCHE, M. WAGNER
Institut für Kernphysik, Technische Universität Darmstadt

## Slide 2: Source of Polarized Electrons at the S-DALINAC
Bulk/Superlattice-GaAs
100 keV electron energy
Vacuum lifetime ~ 1000 h
Charge lifetime 10 (1) C
Polarization 86 (4)%
Emittance ~ 0.15 mm mrad
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 3: Pulsed Electron Beam in the normal conduction Injector
90% beam loss
spin- polarized source
Thermionic gun
To the
S-DALINAC
Differential pumping stage
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 4: Cathode Lifetime
CW-Laser
Pulsed Laser
6 days
Factor 25
Beam Current (mA)
Beam Time (days)
PSTP 2013 - Martin Espig – 13.09.2013
Max. Laser
Power 1 W
Notes: Ein weiteres Problem welches Auftritt ist die Quanteneffizienz der polarisierten Kathode. Diese ist abhängig von der Güte des Vakuums und des während des Betriebes extrahierten Elektronenstroms. Gerade der zweite Punkt sorgt für einen schnellen Abfall der Quanteneffizienz, falls Verluste innerhalb der Strahlführung kompensiert werden müssen. Ist die Quanteneffizienz der Kathode zu klein muss diese neu aktiviert werden, welches einige Stunden in Anspruch nimmt. Typischerweise sollte eine solche Aktivierung höchstens alle 6 Tage durchgeführt werden. In der oberen Grafik sehen Sie daher die maximale Strahlzeit mit einer frisch Präparierten Kathode für den Fall fester Elektronenströme und daraus resultierend erhöhter Laserleistung. Es ist zu erkennen, dass ein Dauerstrichlaser maximal 8µA über 6 Tage liefern kann, während ein gepulster Laser die geforderten 60µA bei 6 Tagen erreicht.

## Slide 5: Pulsed Laser Systems
Mode locked 3 GHz modulated
Ti:Sa-Laser MIRA HP-D External Cavity Diode Laser
→ repetition rate 75 MHz → repetition rate 3 GHz
→ (300-500) fs pulse length → 50 ps pulse length
High Polarization at 780 nm
High Quantum Efficiency at 400 nm
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 6: Reached Electron Bunch Length with the Ti:Sa-Laser at 780 nm
Pulse Compressor: Distance Prism-Grating (cm)
Laser Pulse Length (ps)
4 ps
PSTP 2013 - Martin Espig – 13.09.2013
optical fiber
pulse compressor

## Slide 7: Reached Electron Bunch Length with pulsed Laser Diodes at 780 nm
PSTP 2013 - Martin Espig – 13.09.2013
Electron Bunch Length (ps)
AC/DC
Laser Power (mW)

## Slide 8: Investigation of the Electron Bunches
Electron bunch profile in the time domain
  Intensity vs polarization
  Bulk GaAs vs Superlattice GaAs
  Laser pulse length vs electron bunch length
  Space charge effects
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 9: Measurement of Electron Bunches
spin- polarized source
Thermionic gun
To the
S-DALINAC
Differential pumping stage
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 10: Measurement of Electron Bunches
PSTP 2013 - Martin Espig – 13.09.2013
160 ps

## Slide 11: Comparison Electron Beam Length at 100 keV
Time (ps)
Electron Beam Current (a.u.)
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 12: Comparison Polarization
Bulk-GaAs
Superlattice GaAs
Time (ps)
Time (ps)
Electron Beam Current (nA)
Electron Beam Current (nA)
Mott Scattering Asymmetry
Mott Scattering Asymmetry
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 13: Space Charge Effects
longitudinal
transversal
PSTP 2013 - Martin Espig – 13.09.2013
Bunch Charge (fC)
Bunch Charge (fC)
Bunch Length (ps)
Beam Width (mm)
Notes: Mit Hilfe der Chopper Schlitz Methoden konnten viele Effekte gemessen werden. Ich möchte mich aus zeitmangel hier nur auf die Raumladungseffekte beschränken. In dieser Messung wurde für unterschiedliche Bunchladungen sowohl die Bunchlänge, als auch die transversale Ausdehnung gemessen. In beiden Plots ist einer Vergrößerung ab einer Bunchladung von etwa 1 fC zu erkennen.

## Slide 14: Intensity model by Spicer
Why?
Beam Current (nA)
Time (ps)
Diffusion
Production
Electron transport
Emission
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 15: Particular boundary conditions
Activation problems because of too much oxygen in preparation chamber
  poor activation of cathodes
Poor quantum efficiency
  Low emission probability
  Additional terms may become important
Ansatz for new model
  Include optical recombination
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 16: Advanced Model
A
B
C
direct
SRH
Auger
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 17: Advanced Model
Beam Current (nA)
Time (ps)
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 18: Model for Polarization
BULK GaAs
Superlattice GaAs
SRH-Recombination
Spin-Flip
opt. Recombination
Diffusion
Laser
Preliminary
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 19: Polarization of the Bunch at 100 keV
19
Bulk-GaAs Photocathode
Time (ps)
t = 4,2 ps
1/A = 100 ps
1/A2 = 61,1 ps
B = 1E-10 cm³/s
D = 200 cm²/s
Time (ps)
Beam Current (nA)
Asymmetry
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 20: Polarized Electron Beam at 6.2 MeV
Ag(e,e) Bulk GaAs
top bottom
→ Polarization P ≈ 28%
Channel
Counts/Channel
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 21: Outlook
Repeat measurement of intensity and polarization
  with improved quantum efficiency
  compare with proposed model
Resolution improvement
PSTP 2013 - Martin Espig – 13.09.2013

## Slide 22
Thank you for your attention