## Slide 1: Two Novel Approaches for Electron Beam Polarization from Unstrained GaAs J L McCarter1,2, N B Clayburn3, A Afanasev4, J M Dreiling3, T J Gay3, J Hansknecht5, A Kechiantz4,6, M Poelker5, D M Ryan3
13 September 2013
Charlottesville, VA
1 Department of Physics, University of Virginia, Charlottesville, VA 22901
2 Currently Laser and Plasma Technologies, Hampton, VA 23666
3 Department of Physics, University of Nebraska, Lincoln, NE, 68588
4 Department of Physics, The George Washington University, Washington, DC 20052
5 Thomas Jefferson National Accelerator Facility, Newport News, VA 23606
6 On leave from Institute of Radiophysics and Electronics, NAS of Armenia, Ashtarak 0203, Armenia

## Slide 2: Outline
Motivation: Improve polarization capabilities of the CEBAF photoinjector at Jefferson Lab
  Motivation for higher polarization electron beam
  Brief description of new style micro-Mott polarimeter
  Photoemission from GaAs using two photons
    Theoretical and experimental background
    Current experimental set up
    Electron polarization results and discussion
  Photoemission from GaAs using light with orbital angular momentum
    Theoretical background
    Current experimental set up
    Electron polarization results and discussion
  Future work and questions

## Slide 3: JLab's Electron Beam Needs
Polarized beam currently supplied to 3 experimental halls doing nuclear physics
Interaction statistics go like current*polarization2
Beamtime currently oversubscribed – need to increase polarization
Current 100 keV DC photogun
GaAs photocathode

## Slide 4: Micro Mott for Lab Room Photocathode Experiments
Accelerator-based Mott polarimeters are ~100 keV and require electromagnets: Complicated!
Advantages to operating ~ 20 keV
  Radiation is not an effective problem
  Smaller potentials allow for smaller designs
  Smaller designs usually have increased efficiency, and thus increased figures of merit
  No electromagnets
Sherman function determined by cross calibrating against the 5 MeV Mott @ CEBAF
New design was chosen to have increased efficiency and ease of construction
  Improved efficiency : no
  Ease of construction: YES!

## Slide 5: Electron Source and Polarimeter Apparatus
Three main parts
  Electron Beam Source – Load Locked
  Beam Steering
    Bent 90o, preserving polarization transverse to polarimeter plane
    Simple deflector and polarization rotator
    (Al-Khateeb, H.M. et al., Rev. Sci. Instrum. 1999. 70. 3882)
Incident Laser
Electron Trajectory

## Slide 6: Electron Source and Polarimeter Apparatus
Three main parts
  Electron Beam Source
  Beam Steering
  Mott Polarimeter ( 10” Chamber)
Retarding Field style micro Mott polarimeter
Determined Sherman function by using the same photocathode wafers (bulk and superlattice GaAs) used @ CEBAF and characterized with 5 MeV Mott
Effective Sherman function of 0.201(4) at 20 keV scattering energy

## Slide 7: Photoemission using Two Photons
Nonlinear optical process
Intensity matters! (Power/Area)
      QE proportional to light intensity for two - photon
      QE constant for one - photon
Requires:
  Bulk GaAs
  Light at half the band gap energy of 1.42eV
  Use light at 1560nm instead of 780nm
Two photons are absorbed simultaneously to excite electrons from valance band to conduction band.
QE1560nm very small – need to ensure no photoemission from low wavelengths, where QE is much higher!
  Will vary intensity to verify effects

## Slide 8: Two-Photon Absorption – High Polarization?
Optical transitions in bulk GaAs
  a) one-photon absorption, normal 780nm absorption, ~50% pol
  b) one-photon absorption, strained GaAs, up to 92% pol
  c) two-photon absorption as suggested by Matsuyama et al. Jpn. J. Appl. Phys., 2001, Part 2 40, L555. ~100% pol
Does two photon absorption lead to high (>50%) polarization?

## Slide 9: Other Previous Two-Photon Polarization Results
Previous experimental polarizations disagree
  Pump/probe differential transmission yields
    Pol = 49.5% (Miah, M.I. J. Phys. Chem B. 2009, 113, 6800-6802)
    Pol = 49% (Bhat, R.D.R et al, Phys. Rev. B. 2005, 71, 035209)
  Photoluminescence yields
    Pol = 92% (Suziki, C. et al, Spin 2002 proceedings)
    Pol = 95(3)% (Matsuyama, T. et al, Jpn. J. Appl. Phys. 2001, 40, 555-557)
First to measure polarization via photoemission
  Results coming up…

## Slide 10: QE Characterization of Two-Photon Emission
Equipment
  Polarimeter apparatus previously described
  Bulk GaAs
  Gain switched diode laser at 780nm
  Gain switched diode and fiber amplifier at 1560nm
    Laser has constant average power output regardless of repetition rate of pulses
    Maximum pulse energy was 7 nJ over ~50ps
Measure QE response at 780nm and 1560nm, varying peak intensity: Intensity = Power/Area
  Average power of laser
    In-line optical attenuator
  Repetition rate of pulses
    Repetition rate of laser seed amplifier, pulse width (~50ps)
  Spot size on cathode
    Focusing lenses

## Slide 11: Two-Photon Optical Set Up
l/4
l/2
L
SRD
G
Bias Network
DC Current
G
DFB
ISO
Fiber Amp
RF
LP
Shutter
Translation stages and mirrors
L
LP
Insertable l/2
LPF 850nm
LPFs 1350nm

## Slide 12: GaAs Response to Laser Power
Chart: 780nm
| 1.34 | 1.3260000000000001 | 2.282 | 2.3140000000000001 | 5.1930000000000005 | 5.3679999999999994 | 10.203000000000001 | 10.106 | 21.083000000000002 | 21.078000000000003 | 49.654000000000003 | 49.741999999999997 | 89.975999999999999 | 88.871000000000009 | 150.69200000000001 | 148.88999999999999 | 10.447000000000001 | 10.404999999999999
DC | 1.0301 | 1.0837 | 0.98912 | 1.0249 | 1.1282 | 1.1073 | 1.0631 | 1.1279 | 0.96601 | 0.95496 | 1.0284 | 0.9693 | 0.92557 | 0.92226 | 0.82472 | 0.80951 | 0.97122 | 0.97483
1000 MHz | 1.0047 | 1.0147 | 1.0166 | 1.0113 | 0.98556 | 0.97961 | 0.96831 | 0.9833 | 0.93514 | 0.91895 | 0.86057 | 0.87113 | 0.96619 | 0.94183
500 MHz | 0.96114 | 0.96965 | 0.96072 | 0.96449 | 0.95361 | 0.9508 | 0.93777 | 0.93129 | 0.88517 | 0.89859 | 0.84928 | 0.83165 | 0.91399 | 0.92156
250 MHz | 0.93424 | 0.94238 | 0.94226 | 0.93797 | 0.92251 | 0.94456 | 0.91748 | 0.9023 | 0.86899 | 0.86164 | 0.82763 | 0.82102 | 0.90472 | 0.90008
For 780nm, QE ~ Slight variations seen due to surface charge and space charge effects.
For 1560nm, QE proportional to power, and intensity
Chart: 1560nm
| 7.4127741561928875E-2 | 0.29651096624771628 | 0.42431741721655947 | 0.53380494354653529 | 0.55766214772738598 | 0.71060386738676851 | 0.73701720058699605 | 0.93128300605963776 | 0.92105848998213025 | 1.0292679518024177 | 0.97473719938904446 | 1.2763604236755146 | 1.3049038643918898 | 1.4152434337283244 | 1.4365445088897983 | 1.4459169819608466 | 1.4080010681734232 | 1.5311212826067422 | 1.5481621427359213 | 1.6913053678210259 | 1.722830959060007 | 1.695139561350091 | 1.8915354743388801 | 1.893239560351798 | 1.8753466572161599
250 MHz | 1.53e-08 | 1.1309e-08 | 4.8438e-08 | 6.9598e-08 | 7.0939e-08 | 8.1214e-08 | 8.7963e-08 | 9.1431e-08 | 9.5208e-08 | 1.177e-07 | 1.3189e-07 | 1.4686e-07 | 1.4456e-07 | 1.6106e-07 | 1.5147e-07 | 1.4708e-07 | 1.7354e-07 | 1.9744e-07 | 1.8155e-07 | 2.0091e-07 | 1.7861e-07 | 1.9626e-07 | 1.983e-07 | 1.9082e-07 | 2.0732e-07
500 MHz | 1.2492e-08 | 2.8867e-08 | 2.798e-08 | 4.1753e-08 | 4.1428e-08 | 5.825e-08 | 5.7991e-08 | 7.4182e-08 | 7.5266e-08 | 8.9614e-08 | 9.0567e-08 | 1.1104e-07 | 1.0226e-07 | 1.0717e-07
1000 MHz | 7.3232e-09 | 1.5851e-08 | 1.6467e-08 | 2.6802e-08 | 2.4892e-08 | 3.5608e-08 | 3.5577e-08 | 4.4796e-08 | 4.5291e-08 | 5.7314e-08 | 5.5727e-08 | 5.9348e-08 | 5.7821e-08 | 5.6987e-08
2000 MHz | 6.8623e-09 | 1.1007e-08 | 1.0943e-08 | 1.5995e-08 | 1.5668e-08 | 2.187e-08 | 2.2e-08 | 2.7752e-08 | 2.7928e-08 | 3.5493e-08 | 3.422e-08 | 3.7298e-08 | 3.6873e-08
DC | 4.5085e-10 | 1.2248e-09 | 1.7083e-09 | 2.0937e-09 | 1.7959e-09 | 2.2993e-09 | 3.0099e-09 | 2.89e-09 | 3.8226e-09 | 3.2197e-09 | 4.101e-09 | 4.4189e-09 | 4.3458e-09 | 4.6237e-09 | 4.124e-09 | 3.718e-09 | 4.0692e-09 | 3.8105e-09
Two photon process!

## Slide 13: Bulk Polarization Results
Chart: Electron Polarization in Bulk GaAs
| 1.383875 | 2.6275416666666671 | 2.5929583333333333 | 2.592625 | 2.5603333333333329 | 2.327375 | 2.2703749999999996 | 0.99054166666666665 | 0.97116666666666662 | 1.0292916666666665 | 1.0237500000000002 | 1.0204166666666667 | 1.0315000000000001
780nm | 32.0538 | 32.6433 | 31.8723 | 32.9029 | 32.4183 | 33.2298 | 32.7157 | 31.6626 | 33.8011 | 32.5056 | 33.2554 | 33.8641 | 33.7181
1560nm | 16.5704 | 17.0505 | 17.3754 | 17.371 | 16.6212 | 16.7408 | 17.1158 | 17.8027 | 18.0551 | 16.6135 | 20.1481 | 18.6787 | 16.6924 | 18.7428 | 15.2881 | 17.073 | 16.7666 | 16.7831 | 16.9384 | 17.0681 | 16.1249 | 17.3471 | 13.665
No dependence of measured polarization on extracted photocurrent.
1560nm polarization much lower than predictions/experiments…but why?
At high 1560nm power: start heating wafer – QE falls and lifetime greatly decreases, limiting available photocurrent.

## Slide 14: Investigating Two-Photon Photoemission Polarization Results
Why is the polarization of the extracted beam so much lower than photoluminescence (93%) and differential transmission (49%) experiments?
Unlike previous experiments, photoemitted beam studied.
Absorption coefficient (a) @780nm ~ 1.03x104 cm-1
Effective absorption coefficient (b*Imax) @1560nm ~ 2.5x10-4 cm-1
Electrons must diffuse through more material at 1560nm.
Diffusion introduces depolarization effects.
Used samples of bulk GaAs, with varying active layers, to test the effects these deeper electrons have on polarization.

## Slide 15: GaAs Depolarization Results
Polarization decreases with GaAs thickness, with both two and one photon emission.
 | Photoelectron Polarization % | 
Active Thickness | One-photon (778 nm) | Two-photon (1560 nm)
0.18 mm | 42.6±1.0 | 40.3±1.0
0.32 mm | 44.0±1.1 | 36.0±0.9
Bulk Material | 33.4±0.8 | 16.8±0.4
Max value for two photon polarization (like one photon) seems to be no greater than 50%, making two-photon emission unsuitable for use as a high polarization source.
Chart: Wavelength (nm)
| 777.5 | 1560
Thick Bulk GaAs | 33.4126 | 16.789
.32um Active Layer | 43.9457 | 43.4635 | 41.3154 | 35.9517
.18um Active Layer | 42.612 | 41.9026 | 44.2487 | 40.2685

## Slide 16: Photoemission from OAM Light
Light beams with azimuthal phase dependence can carry orbital angular momentum (OAM).
  OAM light can have arbitrarily large values of angular momentum (±mħ)
  Conventional circularly-polarized light has only one unit (±ħ) of spin angular momentum (SAM) per photon.
Requires:
  Bulk GaAs
  Light at the band gap energy of 1.42eV
  Use linearly polarized light with Laguerre-Gaussian spatial modes to create OAM conditions
QEOAM experimentally approximately the same as QESAM

## Slide 17: OAM Absorption – High Polarization?
Optical transitions in bulk GaAs
  SAM of +1ħ; the circled numbers indicate relative transition strengths
  linearly-polarized light with OAM = +1ħ
  linearly-polarized light with OAM = +2ħ
  linearly-polarized light with OAM = +3ħ
  The dashed arrows correspond to vector addition of SAM of both +1ħ or -1ħ and OAM, as linearly polarized light is composed of photons of both spin states.
Does absorption of OAM light lead to high (>50%) polarization?

## Slide 18: OAM Light Optical Set Up
The diffraction grating can be replaced with gratings of different topological charge to change amount of OAM.
Steering mirrors M1, M2, and M3, and the beam splitter aligned companion OAM beams - verified via the CCD camera.
Mechanical shutters allowed one OAM beam at a time.
Systematic error in polarization associated with beam misalignment, determined by displacing one linearly-polarized beam with a Gaussian profile relative to the other by a distance comparable to the spatial extent of the OAM beams, was 1.8%.
LP
L
Laser
L
Diode
laser
M2
M3
Translation stages and mirrors
CCD
camera
Spatial
filter
Diffraction
grating
Rotatable
l/2
Mechanical
shutters
Beam
splitter
Translation stages and mirrors
Insertable mirror
Vacuum
window
Y
X
Z
Z
X
M1
L
LP
+mħ
-mħ

## Slide 19: OAM Light Production
Intensity patterns of various OAM beams. The integer number m is the topological charge of the vortex. The right most column is the interference pattern obtained by superimposing the positive and negative |m| beams. The interference pattern reveals the order m of the OAM beam.
m = +1
m = -1
|m|=1
Interference
m = +2
m = -2
|m|=2
Interference
m = +3
m = -3
|m|=3
Interference
m = +5
m = -5
|m|=5
Interference
Computer-generated m = 1 interference pattern comprising alternating dark and light fringes. The order-1 fringe defect is in the center of the figure.
FWHM measurements of the focused OAM beams from CCD camera images taken at the same distance from the grating (as measured along the appropriate optical path) as the photocathode.
Topological | Width | Height
Charge | (μm) | (μm)
+1 | 273 | 215
-1 | 313 | 315
+2 | 377 | 436
-2 | 378 | 382
+3 | 488 | 443
-3 | 536 | 495
+5 | 719 | 745
-5 | 842 | 680

## Slide 20: Measured OAM Electron Asymmetry
Asymmetry as a function of Δfor OAM light and circularly polarized light. Solid and dashed lines indicate the weighted linear fit for extrapolation to ΔE = 0 eV for OAM and circularly polarized light respectively. Statistical error bars are smaller than the data points.

## Slide 21: Measured Polarization and Systematic Error
For beams with opposite degrees of OAM, the locations of maximum intensity shifted ~ 90o.
Electron transmission between the photocathode to the polarimeter was highly dependent on the incident laser location.
Complementary OAM states had slightly different transmission rates and beam trajectories to the polarimeter, introducing the dominant systematic error.
m = +2
m = -2
m = +5
m = -5
The systematic error associated with beam misalignment, determined by displacing one linearly-polarized beam with a Gaussian profile relative to the other by a distance comparable to the spatial extent of the OAM beams, was 1.8%.
Standard asymmetry calculation does not normalize for different detection rates on the same detector over different polarization states.

## Slide 22: OAM Polarization Results
Electron polarization produced by light with varying degree of OAM. Composite errors are shown.
Dependence of electron polarization on laser spot size incident on the photocathode for OAM light. Composite errors are shown.
Sadly, the polarization of electrons created via OAM light is lower than 2.5%, compared to 35% polarization with circularly polarized light. Given the systematic spatial displacement, these results are consistent with zero, suggesting no coupling of OAM to the extended (delocalized) electron states in GaAs, at least with beams of diameter >250 mm.
Dependence of electron polarization on the angle of linear light polarization incident on the photocathode. The large error bar includes the composite (systematic and random) error of the asymmetry measurement as well as the error in Seff. Subsequent error bars exclude systematic error.

## Slide 23: The End
Any questions?
Comments?

## Slide 24: Comparison to other Mott designs
Paper | Institution | Year | Target | Voltage (keV) | Max. Efficiency (x 0.001) | Max. Sherman (%) | Max. FOM (x 0.0001)
Neufeld | Rice | 2007 | Th | 25 | 6 | 25 | 1.2
Snell | Rice/ALS | 2000 | Au | 25 |  |  | ~1
Tang | Rice | 1988 | Au | 20 | 2 | 10.5 | 
Iori | Hiroshima | 2006 | Au | 20 | 9.9 | 13 | 1.7
Iori | Hiroshima | 2006 | Au | 25 | 13 | 12 | 1.8
Iori | Hiroshima | 2006 | Au | 30 | 8.3 | 15 | 1.9
Uhrig | Muenster | 1989 | Au | 20 | 0.01 | 25 | 0.006
Petrov | St. Petersburg | 1997 | Au | 60 |  | 33 | 2.5
Petrov | St. Petersburg | 2003 | Au | 40 |  | 32 | 5.6
McCarter | Jlab/UVA | 2009 | Au | 20 | 0.6 | 20.1 ± .4 | 0.011

## Slide 25: Surface Uniformity of GaAs
QE of GaAs surface not uniform, due to positioning of Cs and NF3 sources
Transmission to microMott is very dependent on initial laser positioning on the cathode.
Care must be taken during experiments to ensure continuity of QE and transmission states during taking of data.
Chart: QE %, 780nm
| 0 | 0.63500000000000345 | 1.27 | 1.905 | 2.54 | 3.1749999999999998 | 3.8099999999999987 | 4.4450000000000003 | 5.08 | 5.7149999999999945 | 6.35 | 6.9850000000000003 | 7.6199999999999966 | 8.2550000000000008 | 8.89 | 9.5250000000000004 | 10.16 | 10.795 | 11.43 | 12.065000000000024 | 12.7 | 13.335000000000004 | 13.97 | 14.605
2.54 | 0.0013471 | 0.0015653 | 0.0018663 | 0.0024157 | 0.0025286 | 0.0029951 | 0.0037703 | 0.0044175 | 0.0050345 | 0.0057269 | 0.0057344 | 0.0057796 | 0.0054259 | 0.0047937 | 0.0042444 | 0.002807 | 0.0027995 | 0.0021147 | 0.0018061 | 0.0016707 | 0.0015427 | 0.0017459 | 0.0017685 | 0.0028446
3.175 | 0.0015653 | 0.0018738 | 0.0024608 | 0.0035069 | 0.0040337 | 0.0045153 | 0.0063816 | 0.0078416 | 0.0085866 | 0.010889 | 0.011266 | 0.011281 | 0.0096477 | 0.0091058 | 0.0081953 | 0.0049894 | 0.0045454 | 0.0036122 | 0.0025511 | 0.0018964 | 0.0017384 | 0.0016105 | 0.0016105 | 0.0016105
3.81 | 0.0019265 | 0.002506 | 0.0031381 | 0.0053205 | 0.0054108 | 0.0069385 | 0.013072 | 0.014155 | 0.03245 | 0.21402 | 0.21621 | 0.23487 | 0.23043 | 0.16089 | 0.05912 | 0.020198 | 0.0096853 | 0.0064493 | 0.0044175 | 0.0031607 | 0.0024307 | 0.0017685 | 0.001761 | 0.0016255
4.445 | 0.0028898 | 0.0034391 | 0.0043949 | 0.0074201 | 0.0074653 | 0.010498 | 0.11701 | 0.27069 | 0.93497 | 1.2674 | 1.2689 | 1.4124 | 1.3568 | 1.2239 | 0.79386 | 0.13969 | 0.058029 | 0.0069159 | 0.0048389 | 0.0048539 | 0.0033564 | 0.0027092 | 0.0021598 | 0.0017384
5.08 | 0.0034316 | 0.0052227 | 0.0056817 | 0.010664 | 0.010709 | 0.086648 | 0.60001 | 1.1035 | 1.2312 | 1.3026 | 1.2954 | 1.3491 | 1.36 | 1.3582 | 1.3705 | 1.0207 | 1.0224 | 0.026302 | 0.021741 | 0.0077588 | 0.0052829 | 0.0027393 | 0.0027242 | 0.0021749
5.715 | 0.0046432 | 0.005614 | 0.0073976 | 0.11977 | 0.12124 | 0.70107 | 1.0194 | 1.0487 | 1.0542 | 1.1084 | 1.1321 | 1.1408 | 1.1586 | 1.1592 | 0.96755 | 1.1496 | 1.1342 | 0.85437 | 0.03169 | 0.020703 | 0.0072621 | 0.003537 | 0.003409 | 0.0024985
6.35 | 0.0058473 | 0.0063816 | 0.0085188 | 0.63839 | 0.63816 | 0.94776 | 0.91322 | 0.90148 | 0.93128 | 0.91164 | 0.89508 | 0.92037 | 0.88515 | 0.92082 | 0.92797 | 0.9519 | 0.84391 | 0.56569 | 0.69152 | 0.3631 | 0.0064042 | 0.0046282 | 0.0032059 | 0.0032284
6.985 | 0.006359 | 0.0071567 | 0.02302 | 0.75308 | 0.79311 | 0.75699 | 0.68979 | 0.6928 | 0.65705 | 0.67556 | 0.69377 | 0.68866 | 0.70281 | 0.69039 | 0.70777 | 0.5468 | 0.51595 | 0.7682 | 0.78942 | 0.85173 | 0.12077 | 0.005471 | 0.0054786 | 0.0039057
7.62 | 0.0071342 | 0.19408 | 0.20815 | 0.65427 | 0.65728 | 0.62191 | 0.57841 | 0.5179 | 0.54733 | 0.54951 | 0.57698 | 0.60302 | 0.57713 | 0.57231 | 0.55327 | 0.31961 | 0.31758 | 0.63191 | 0.65509 | 0.80447 | 0.01268 | 0.0061333 | 0.0061408 | 0.0045905
8.255 | 0.0083006 | 0.029252 | 0.41247 | 0.55922 | 0.55455 | 0.49247 | 0.46997 | 0.46921 | 0.45477 | 0.47049 | 0.48035 | 0.50925 | 0.49239 | 0.49593 | 0.437 | 0.30027 | 0.30508 | 0.39027 | 0.57638 | 0.6873 | 0.48216 | 0.0063289 | 0.0064644 | 0.0048615
8.89 | 0.030094 | 0.14149 | 0.5085 | 0.43731 | 0.4428 | 0.41744 | 0.39727 | 0.38779 | 0.41586 | 0.41924 | 0.43896 | 0.43573 | 0.41435 | 0.38892 | 0.31298 | 0.33473 | 0.34753 | 0.47027 | 0.53393 | 0.60008 | 0.53619 | 0.0061032 | 0.0058925 | 0.0046658
9.525 | 0.12076 | 0.18874 | 0.39893 | 0.35701 | 0.35934 | 0.34851 | 0.35596 | 0.34873 | 0.35814 | 0.33925 | 0.35866 | 0.33677 | 0.27709 | 0.27302 | 0.20966 | 0.3254 | 0.3239 | 0.4273 | 0.45612 | 0.55056 | 0.016977 | 0.016993 | 0.0056215 | 0.0044551
Chart: Distance (mm)
| 0 | 0.63500000000000345 | 1.27 | 1.905 | 2.54 | 3.1749999999999998 | 3.8099999999999987 | 4.4450000000000003 | 5.08 | 5.7149999999999945 | 6.35 | 6.9850000000000003 | 7.6199999999999966 | 8.2550000000000008 | 8.89 | 9.5250000000000004 | 10.16 | 10.795 | 11.43 | 12.065000000000024 | 12.7 | 13.335000000000004 | 13.97 | 14.605
2.54 | 0.00010171 | 0.00010171 | 0.00015256 | 0.00015256 | 5.0855e-05 | 5.0855e-05 | 5.0855e-05 | 0.00020342 | 0.00020342 | 5.0855e-05 | 5.0855e-05 | 0.00020342 | 0.00010171 | 0.00010171 | 0.00010171 | 0.00010171 | 0.00010171 | 5.0855e-05 | 5.0855e-05 | 0 | 0.00020342 | 0.00015256 | 0.00015256 | 0.00010171
3.175 | 0.00025427 | 0 | 0.00025427 | 0.00010171 | 0.00015256 | 0.00030513 | 0.00015256 | 5.0855e-05 | 0.00025427 | 0.00025427 | 5.0855e-05 | 0.00010171 | 0.00020342 | 0.00025427 | 0.00015256 | 0.00020342 | 0.00015256 | 0.00015256 | 0.00010171 | 0.00010171 | 0.00010171 | 0 | 0.00015256 | 5.0855e-05
3.81 | 0.00020342 | 0.00025427 | 0.00010171 | 0.00035598 | 0.00030513 | 0.00010171 | 0.00040684 | 0.00030513 | 0.00025427 | 0.00045769 | 0.00025427 | 0.00025427 | 0.00025427 | 5.0855e-05 | 0.00025427 | 0.00030513 | 0.00015256 | 0.00025427 | 5.0855e-05 | 0.00010171 | 0.00010171 | 0.00010171 | 0 | 0
4.445 | 0.00025427 | 0 | 0.00040684 | 0.00040684 | 0.00015256 | 0.00020342 | 0.0005594 | 0.00045769 | 0.00066111 | 0.00030513 | 0.00025427 | 0.00015256 | 0.00035598 | 0.0005594 | 0.00035598 | 0.00035598 | 0.00020342 | 0.00015256 | 0.00010171 | 0.00010171 | 0.00010171 | 0 | 0.00015256 | 0.00010171
5.08 | 0.00040684 | 0.00045769 | 0.00030513 | 0.00035598 | 0.00015256 | 0.00050855 | 0.00050855 | 0.00030513 | 0.00020342 | 0.00010171 | 0.00010171 | 0.00015256 | 0.00010171 | 0.00035598 | 0.00015256 | 0.00045769 | 0.00061026 | 0.00045769 | 0.00010171 | 5.0855e-05 | 0.00010171 | 0.00010171 | 0.00020342 | 0.00010171
5.715 | 0.00040684 | 0.00030513 | 0.00035598 | 0.00040684 | 0.00020342 | 0.00050855 | 0.00050855 | 0.00025427 | 0.00035598 | 0.00030513 | 0.00030513 | 0.00025427 | 0.00020342 | 0.00025427 | 0.00015256 | 0.00030513 | 0.00040684 | 0.00081368 | 0.00061026 | 0.00025427 | 0.00020342 | 0.00020342 | 5.0855e-05 | 0.00020342
6.35 | 0.00045769 | 0.00030513 | 0.00040684 | 0.00076282 | 0.0012714 | 0.00076282 | 0.0005594 | 0.00061026 | 0.00076282 | 0.00045769 | 0.00030513 | 0.00040684 | 0.00025427 | 0.00020342 | 0.00025427 | 0.00010171 | 0.00030513 | 0.00035598 | 0.0016782 | 0.00045769 | 5.0855e-05 | 0.00010171 | 0.00020342 | 5.0855e-05
6.985 | 0.00045769 | 0.00050855 | 0.0026953 | 0.0042718 | 0.0033564 | 0.0019325 | 0.0014239 | 0.0005594 | 0.00071197 | 0.00045769 | 0.0005594 | 0.00010171 | 0.00015256 | 0.00020342 | 0.00020342 | 0.00015256 | 5.0855e-05 | 0.00015256 | 0.00096624 | 0.0014748 | 0.00050855 | 0.00010171 | 0.00010171 | 0
7.62 | 0.00071197 | 0.0019325 | 0.015714 | 0.01368 | 0.0091539 | 0.0053906 | 0.0028479 | 0.0019833 | 0.001068 | 0.0005594 | 0.00076282 | 0.00061026 | 0.00040684 | 0.00035598 | 0.00035598 | 0.00025427 | 0.00035598 | 0.00020342 | 0.00035598 | 0.0023393 | 0.0015765 | 0.00020342 | 0.00010171 | 0.00020342
8.255 | 0.00071197 | 0.0090522 | 0.028631 | 0.025275 | 0.015867 | 0.0099167 | 0.0054415 | 0.0027462 | 0.0016274 | 0.00086453 | 0.00086453 | 0.0005594 | 0.00035598 | 0.00045769 | 0.00025427 | 0.00035598 | 0.00015256 | 5.0855e-05 | 0.00035598 | 0.0011188 | 0.0013222 | 0.00010171 | 0 | 5.0855e-05
8.89 | 0.0030513 | 0.018867 | 0.032293 | 0.030208 | 0.023851 | 0.019833 | 0.015409 | 0.010425 | 0.0038141 | 0.0016274 | 0.00081368 | 0.00091539 | 0.00045769 | 0.00040684 | 0.00020342 | 0.00030513 | 0.00010171 | 0 | 0.00010171 | 0.00025427 | 0.0005594 | 0.00030513 | 5.0855e-05 | 0.00015256
9.525 | 0.0033564 | 0.016935 | 0.031937 | 0.03809 | 0.044854 | 0.073282 | 0.10344 | 0.071197 | 0.025071 | 0.006662 | 0.0022376 | 0.0014239 | 0.00076282 | 0.00061026 | 0.00050855 | 0.00020342 | 5.0855e-05 | 0.00025427 | 0.00015256 | 0.00020342 | 0.00096624 | 0.00066111 | 0.00015256 | 0.00010171
Transmission %
Mott current/photocurrent

## Slide 26: Polarimeter Characteristics
Chart: Incident Scattering Energy (keV)
| 5 | 10 | 15 | 20 | 25 | 30
Bulk | 0.066 | 0.13767 | 0.17033 | 0.1975 | 0.21217 | 0.23117
Superlattice | 0.062857 | 0.14238 | 0.17345 | 0.19405 | 0.20935 | 0.22821
Determined Sherman function by using same piece materials (bulk and superlattice GaAs) used @ CEBAF and characterized with 5 MeV Mott
Value of 0.201(4) at 20 keV scattering energy
Chart: Energy (keV)
| 5 | 10 | 15 | 20 | 25 | 30
 | 1.4052 | 1.1035 | 0.80453 | 0.60623 | 0.47647 | 0.391
Efficiency of 0.6x10-3 and a FOM of 0.011x10-4 at 20keV scattering energy.
Efficiency is ~order of magnitude lower than comparable designs
Still useful, only need ~100 pA to target